| BOILING POINT (INITIAL): | 207-237°C | SPECIFIC GRAVITY: | 0.88 typical at 21°C |
| --- | --- | --- | --- |
| SOLUBILITY IN WATER: | Insoluble | pH: | Not Applicable |
| VAPOR PRESSURE: | Not determine | VAPOR DENSITY: | >1 |
|  |  | VOC: | Not determine |
| COEFFICIENT OF WATER/OIL DISTRIBUTION: | Not determine | APPEARANCE/ODOR: | Light amber liquid with a mild petroleum odor. |
| FLASHPOINT: | >83°C | FLAMMABLE LIMITS: | LEL: 0.6% UEL: 9.5% |

TECHNICAL DATA SHEET

WD-40 Specialist®

SPRAY & STAY

| Product Description |  | PACKAGING |
| --- | --- | --- |
| WD-40 Specialist Spray & Stay No-Drip Formula offers 12x longer-lasting lubrication when compared to WD-40® Multi-Use Product. It has been designed for superior protection that resists water and displaces moisture to prevent rust for up to one year.** This product sets into a gel that stays where you spray, making it ideal for use on vertical surfaces and offers non-fling for moving parts such as gears, bearings, cables, chains, rollers and more. Once applied withstands temperature ranges from -55°C to +200°C. Safe on multiple surfaces including metals, most plastics, and most rubbers. |  |  |
| Applications | Features & Benefits |  |
| - Chains - Cables - Gears - Rollers - Bearings - Vertical Surfaces - Moving Parts | - No Drip - No Mess - Unique, Thick Gel Lubricant - 12x Longer-Lasting Lubrication* - Prevents rust for up to 1 year** - Effective in a temperature Ranges from -55°C to +200°C * Compared to WD-40 Multi-Use Product ** Results may vary depending on extreme conditions |  |
| fluid Properties |  |  |

Packaging Specifications

SKU Codes and Description; Individual Item (Consumer Unit); Carton (Traded Unit); Pallet Information. Case Codes; Unit Codes; Product Description; Dimensions (mm); Cubic Volume (cm³); Gross Weight (kg); Dimensions (mm); Cubic Volume (cm³); Gross Weight (kg); Units Per Carton; Consumer Units Per Pallet; Dimensions (mm); Gross Weight (kg). Width; Depth; Height; Width; Depth; Height; Width; Depth; Height. 21124; 21027; WD-40 Specialist Spray & Stay Gel Lubricant 300g Smart Straw; 66; 66; 245; 1067; 0.43; 137; 200; 252; 6905; 2.69; 6; 1008; 1165; 1165; 1158; 485.92.

Direction

Shake can well for 20-30 seconds before each spray. Flip straw up for narrow spray or down for wide spray. Spray on surface to be lubricated or protected ensuring full coverage for maximum protection.

hazard identification

HAZARDOUS SUBSTANCE. DANGEROUS GOODS. According to the WHS Regulations and the ADG Code. DANGER! Extremely flammable aerosol. Pressurized container: may burst if heated. May be fatal if swallowed and enters airways. Repeated exposure may cause skin dryness or cracking. Keep away from heat, hot surfaces, sparks, open flames and other ignition sources. No smoking. Do not spray on an open flame or other ignition source. Do not pierce or burn, even after use. If swallowed: Immediately call a POISON CENTER or doctor. DO NOT induce vomiting. If discomfort persists, see a doctor. Additional information is listed in the safety data sheet.

Storage

Store in a cool, dry ventilated area away from incompatible materials. Protect from physical damage. Do not store in direct sunlight, near open flames or above temperatures greater than 50°C.

Regulatory Information

Montreal Protocol (Ozone Depleting Substances): None present. The Stockholm Convention (Persistent Organic Pollutants): None present. The Rotterdam Convention (Prior Informed Consent): Not applicable. Basel Convention: Not applicable. International Convention for the Prevention of Pollution from Ships (MARPOL): Not applicable. Standard for the Uniform Scheduling of Medicines and Poisons (SUSMP): Not applicable Australian Inventory of Chemical Substances: All the components of this product are listed on the AICS inventory New Zealand Inventory: All the ingredients comply with the HSNO regulations

WD-40 Specialist®

SPRAY & STAY

Level 2, 41 Rawson Street, Epping, NSW 2121 Australia		         Version: 1.0

wd40.com.au

TECHNICAL DATA SHEET